Meddling with Metals, Part 2

Teacher notes

- Time needed to complete lab: Approximately two 45 minute class periods.

- Target grade level: middle school to high school; chemistry or physics

- Objectives: Students will be able to describe how metals change under different heating processes. Students will be able to determine which heating process they would use to change a metal’s properties to suit a specific use.

- Major concepts: Heating changes a metal’s properties.

- Preparation: Pour enough bb’s into a petri dish to just cover the bottom. Cover the dish and seal the edges with tape.

- Typical results or sample data:

Data Table 1: Number of Bends until Bobby Pin Breaks

|  | 1st trial | 2nd trial | 3rd trial | average |
| --- | --- | --- | --- | --- |
| Control | 4 | 5 | 4 | 4.33 bends |
| Annealing | 12 | 11 | 11 | 11.33 bends |
| Quenching | 1 | 1 | 1 | 1 bends |
| Tempering | 6 | 8 | 8 | 7.33 bends |

Data Table 2: Number of Bends until Brass Welding Rod Breaks

|  | 1st trial | 2nd trial | 3rd trial | average |
| --- | --- | --- | --- | --- |
| Control |  |  |  |  |
| Annealing |  |  |  |  |
| Quenching |  |  |  |  |
| Tempering |  |  |  |  |

- Answers to questions:

How does heating a metal change its properties?

Heating a metal changes its properties because it allows the atoms and molecules to ‘relax’ and slide past each other. This also creates distortions in the metal, which can affect the