Playing With Polymers: Polymer Balls

Teacher Notes

Time Needed to Complete the Lab:  About 1½ hours

Target Grade Level:  7th-12th grade depending on the complexity of extension activities

Objectives:

- Prepare three types of polymer balls in the laboratory

- Investigate and compare the physical properties of the polymer balls

- Discuss the bonding and cross linking of polymers.

Major Concepts:

Polymers, cross linking, condensation polymerization, density, translucence, opacity, kinetic energy, potential energy, volume

Preparation Tips:

- The acetic acid, latex, and ethanol should be in a working fume hood till students measure out the quantities they need.

- Students should work in a well-ventilated area.

- The volume of the polymer balls should be calculated using the diameter, because sodium silicate dissolves in water.

- To measure bounce height, have students drop the ball from the same height (1 meter).

Sample Data:  Polymer Ball #2

- Appearance of the ball:  Rubbery (can be used as an eraser).

- Elasticity of the ball:  Very elastic; bounces back when stretched.

- Shape of the ball:  Holds its shape; difficult to reshape.

| Trial # | Bounce Height (cm) | Bounce Time (s) | Mass (g) | Diameter (cm) |
| --- | --- | --- | --- | --- |
| 1 | 40 | 2.50 | 5.43 | 2.25 |
| 2 | 45 | 2.52 | 5.43 | 2.35 |
| 3 | 43 | 2.63 | 5.43 | 2.30 |
| Average | 43 | 2.55 | 5.43 | 2.30 |

Sample Calculations:

- Volume of ball #2 = 6.37 cm3

- Density of ball #2 = 0.85 g/cm3

Additional References:

http://chemistry.about.com/od/demonstrationsexperiments/ss/bounceball.htm

http://chemistry.about.com/od/chemistryactivities/Chemistry_Activities_for_Kids.htm

Extension Activities:

- Investigate the structural formulas for each of the monomers used in the formation of the polymer balls in this activity, and describe the chemical reaction.

- Compare the properties of the polymer balls prepared in the lab with commercial polymer balls.

- Use motion detectors and graphing calculators to use high-tech tools and analyze bounce height.

Vocabulary

Polymer:  A compound made up of monomers bonded together in long chains.

Elastomer:  A polymer that is able to retain its form after undergoing deformation.

Condensation:  A reaction in which a small molecule is removed when two molecules bond together to form a larger molecule.

Polymerization:  The process of making long polymeric chains.

Density:  Mass of a substance per unit volume of that substance.

Mass:  The amount of matter in a substance.

Volume:  The space occupied by a substance.

Translucent:  The property of allowing some light through.

Opaque:  The property of not allowing light through.